## Slide 1: Modeling of high-strength steels (HSS) in automobile forming (DP1000)
Group 5: An Mai, Thoa Le, Hoang Le, Linh Nguyen
Advisor: Li Zinan
Supervisor: Junhe Lian
Aalto University, Finland
Notes: high strength and hierarchical bcc microstructure

## Slide 2: Table of Contents
Introduction
Methodology
  Brief recap of working flow and recap
Constitutive model
  Temperature calibration
  Strain-rate calibration
Machine learning
  Methodology
Validation
  Constitutive model
  Machine learning model
Discussion and conclusion
  Comparison between constitutive model and machine learning model
  Results summary

## Slide 3: Introduction
An overview of the hot stamping process sequence. Naderi et al, 2011
Picture of hot forming and cold forming vehicle parts. Chang, Meng, et al, 2011
* Advanced steel applications in a modern car body structure. Asghari et al, MSEA 2013.

## Slide 4: Table of Contents
Introduction Motivation --An
Methodology --An
  Brief recap of working flow
  Recap first half progress: Constitutive + ML
Constitutive model
  Temperature calibration: How + results --Thoa
  Strain-rate calibration: How + result --Linh
  Validation --An
Machine learning --Hoang
  How + results
  Validation: 500C with simulation
Discussion + Conclusion
  Summary of final results + compare with the existing paper -- Thoa
  Comparison -- Linh
  Conclusion: Lesson learnt

## Slide 5: Methodology
Uniaxial tensile test
Flow fitting curve
1
ML-coupled model
2
3
Abaqus simulation
4
Fracture test
6
5
6
StrRtDpn & TmpDpn params calibration

## Slide 6: Recap of first half progress
Uniaxial tensile tests 43 cases on DP1000 (DD,RD,TD,Tmpt, StrnRt)

## Slide 7: Recap of first half progress
Uniaxial tensile tests:
  What has been done:
  Process data
  Graph strain-rate dependent and temperature dependent flow curves

## Slide 8: Recap of first half progress
6
Uniaxial tensile test
Flow fitting curve
1
ML-coupled model
2
3
Abaqus simulation
4
Fracture test
5
6
StrRtDpn & TmpDpn params calibration

## Slide 9: Recap of first half progress
ML-coupled for temperature and strain-rate dependence
  What has been done:
    Built an LSTM Machine Learning model.
    Used 8 flow curves for training, 12 for testing

## Slide 10: Recap of first half progress
ML-coupled for temperature and strain-rate dependence
  What has been done:
    Built an LSTM Machine Learning model.
    Used 8 flow curves for training, 12 for testing
    Training results: R-squared > 0.985

## Slide 11: Recap of first half progress
ML-coupled for temperature and strain-rate dependence
  What has been done:
    Built an LSTM Machine Learning model.
    Used 8 flow curves for training, 12 for testing
    Training results: R-squared > 0.985
    Testing results are not are not good

## Slide 12: Recap of first half progress
6
Uniaxial tensile test
Flow fitting curve
1
ML-coupled model
2
3
Abaqus simulation
4
Fracture test
5
6
StrRtDpn & TmpDpn params calibration

## Slide 13: Recap of first half progress
Flow fitting curve
What has been done?
Extend experimental data until strain value of 3
Use curve_fit() function to find parameters for S-V equation for lower strain rates, and modify S-V equation at higher strain rates

## Slide 14: Recap of first half progress
Flow fitting curve
What has been done?
Extend experimental data until strain value of 3
Use curve_fit() function to find parameters for S-V equation for lower strain rates, and modify S-V equation at higher strain rates
Use curve_fit() for the r-value fitting

## Slide 15: Recap of first half progress
6
Uniaxial tensile test
Flow fitting curve
1
ML-coupled model
2
3
Abaqus simulation
4
Fracture test
5
6
StrRtDpn & TmpDpn params calibration

## Slide 16: Methodology
4. Abaqus simulation
DP material properties including strain, stress in RD,TD,DD, biaxial direction, r-values (Lankford coefficients).
Loading direction for 5 geometries
VUMAT subroutine
5. Fracture tests – Force and Displacement curve
Reference
Reference

## Slide 17: Recap of first half progress
What has been done?
Use data of flow curves along 0, 45, 90, biaxial and r-values along 3 loading direction to make material input files.
Run Abaqus simulation: 305 cases.
Run ODB files through Abaqus CAE to obtain force-displacement data
Plot simulated data and experimental data to validate

## Slide 18: Current objectives
6
Flow fitting curve
1
2
3
4
Fracture test
5
6
Uniaxial tensile test
Flow fitting curve
1
ML-coupled model
2
3
Abaqus simulation
4
Fracture test
5
6
StrRtDpn & TmpDpn params calibration

## Slide 19: Constitutive model – Introduction
Stress function
Strain effect
Temperature effect
Strain-rate effect
Flow stress
Reference stress
Study temperature / strain-rate and stress relationship
Define reference stress
Develop equations
Develop parameter equations
Fitting validation
Simulation validation
Thermal softening
Dynamic strain aging
Adiabatic heat
Fixed stress

## Slide 20: Constitutive model – Temperature parameters calibration
Given 6-parameter equation
F. Shen, et al.2020,Int. J. Plasy.
Proposed 9-parameter equation
Thermal Softening Dynamic Strain Aging
Thermal Softening Dynamic Strain Aging
Less accurate at some strains
Depends significantly on initial guesses, and extensive iterations were required to achieve satisfactory results
More complicated
More accurate
Less dependent on initial guesses

## Slide 21: Constitutive model – Temperature parameters calibration
Strain-rate 0.0001
Smallest R-squared value: 0.971
Largest R-squared value: 1
Average value: 0.994
R-squared values > 0.99: 99.75%
Strain-rate 0.001
Smallest R-squared value: 0.685
Largest R-squared value: 1
Average value: 0.998
R-squared values > 0.99: 98.48%
Given 6-parameter equation
F. Shen, et al.2020,Int. J. Plasy.

## Slide 22: Constitutive model – Temperature parameters calibration
Strain-rate 0.01
Smallest R-square value: 0.87
Largest R-square value: 1
Average value: 0.996
R-square values > 0.99: 84.81%
Strain-rate 0.1
Smallest R-square value: 0.449
Largest R-square value: 1
Average value: 0.987
R-square values > 0.99: 94.94%
Given 6-parameter equation
F. Shen, et al.2020,Int. J. Plasy.

## Slide 23: Constitutive model – Temperature parameters calibration
Proposed 9-parameter equation
Strain-rate 0.0001
Smallest R-squared value: 0.99
Largest R-squared value: 1
Average value: 1
R-squared values > 0.99: 100%
Strain-rate 0.001
Smallest R-squared value: 0.483
Largest R-squared value: 1
Average value: 0.998
R-squared values > 0.99: 99.24%

## Slide 24: Constitutive model – Temperature parameters calibration
Proposed 9-parameter equation
Strain-rate 0.01
Smallest R-squared value: 0.975
Largest R-squared value: 1
Average value: 0.999
R-squared values > 0.99: 97.47%
Strain-rate 0.1
Smallest R-squared value: 0.91
Largest R-squared value: 1
Average value: 1
R-squared values > 0.99: 99.75%

## Slide 25: Constitutive model – Temperature parameters calibration
Proposed equation vs given equations
R-squared | Strain-rate 0.0001 |  | Strain-rate 0.001 |  | Strain-rate 0.01 |  | Strain-rate 0.1 | 
Function | 6-parameter | 9-parameter | 6-parameter | 9-parameter | 6-parameter | 9-parameter | 6-parameter | 9-parameter
Smallest value | 0.971 | 0.99 | 0.685 | 0.483 | 0.87 | 0.975 | 0.449 | 0.91
Largest value | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1
Average value | 0.994 | 1 | 0.998 | 0.998 | 0.996 | 0.999 | 0.987 | 1
R-squared values > 0.99 | 99.75% | 100% | 98.48% | 99.24% | 84.81% | 97.47% | 94.94% | 99.75%
The 9-parameter function provides higher accuracy and greater consistency.

## Slide 26: Constitutive model – Temperature parameters calibration
Proposed 9-parameter equation
Given 6-parameter equation
One function for all parameters
Parameter calibration
The trend varies significantly across different strain rates
It is manageable to calibrate parameters for strain rate 0.0001
=> Parameters evolving with strain
Continue to calibrate C parameter

## Slide 27: Constitutive model – Temperature parameters calibration
Thermal parameters C1 – C6 calibration (for Strain rate 0.0001)
Low strain: Initial rapid changes (first Gaussian and decay).
Intermediate strain: Subsequent rises and peaks (second Gaussian).
Large strain: Final stabilization or leveling off (logistic function).
C1
C2
C3

## Slide 28: Constitutive model – Temperature parameters calibration
Thermal parameters C1 – C6 calibration (for Strain rate 0.0001)
C4
C5
C6
 | C1 | C2 | C3 | C4 | C5 | C6
R-squared value | 0.998 | 0.996 | 0.99 | 0.974 | 0.996 | 0.915

## Slide 29: Constitutive model – Temperature parameters calibration
Stress validation result
Average R-squared value: 0.973
R-squared values > 0.9: 96.46%
From strain 0.012, fitting quality is improved
The model is validated

## Slide 30: Constitutive model – strain-rate dependent parameters calibration
Stress function
Strategy
Study temperature / strain-rate and stress relationship
Define reference stress
Develop equations
Develop parameter equations
Fitting validation
Simulation validation
Flow stress

## Slide 31: Constitutive model – strain-rate dependent parameters calibration
Experimental data
Strain-rate dependency varies greatly between temperatures.
Temperature affects thermal activation, deformation mechanisms and microstructural evolution.
Notes: Thermal Activation: Higher temperatures enhance atomic motion, reducing resistance to deformation and increasing strain-rate sensitivity.
Deformation Mechanisms: Dominant mechanisms (e.g., dislocation glide, creep) vary with temperature, altering stress-strain behavior.
Microstructural Evolution: Temperature impacts grain structure, phase transformations, and recovery processes, driving differences in strain-rate dependency.
-

## Slide 32: Constitutive model – strain-rate dependent parameters calibration
Given equations
Power-law (Kleemola, H.J. and Ranta-Eskola, A.J., 1979)
Wagoner (Wagoner, R.H., 1981)
Past student’s proposal
=> Assume simple linear or logarithmic relationship between normalized stress and strain
Notes: Power-law and Wagoner: If your data shows a more complex stress-strain rate behavior (e.g., non-linear trends, asymptotes, or transitions at extreme strain rates), these models cannot accommodate such behaviors. This is because they rely solely on simple mathematical forms (power-law and square-root terms) and lack terms like quadratic or logarithmic contributions.
Student: Assume that the relationship between stress and strain rate (after normalization) is nearly linear or a simple logarithmic function. If the data shows deviations or bending patterns that cannot be captured by a linear-log or power-law model.

## Slide 33: Constitutive model – strain-rate dependent parameters calibration
Proposed equation
Tmp 298.15K – 25C
Smallest R-squared value: 0.968
Largest R-squared value: 1
Average value: 0.993
R-squared values > 0.98: 91.76%
Tmp 373.15K – 100C
Smallest R-squared value: 1
Largest R-squared value: 1
Average value: 1
R-squared values > 0.98: 100%
Notes: - Non-linear Scaling of Strain Rate: Limited representation of the strain rate’s influence
- Higher Flexibility Through Quadratic Term: Account for curvature or non-linear behavior in the stress-strain rate relationship. In situations where the stress-strain rate curve has a “hump” or inflection point, your function can adjust the curvature through the quadratic term.

## Slide 34: Constitutive model – strain-rate dependent parameters calibration
Proposed equation
Tmp 473.15K – 200C
Smallest R-squared value: 1
Largest R-squared value: 1
Average value: 1
R-squared values > 0.98: 100%
Tmp 573.15K – 300C
Smallest R-squared value: 1
Largest R-squared value: 1
Average value: 1
R-squared values > 0.98: 100%
Tmp 673.15K – 500C
Smallest R-squared value: 0.975
Largest R-squared value: 1
Average value: 0.999
R-squared values > 0.98: 98.82%

## Slide 35: Constitutive model – strain-rate dependent parameters calibration
Proposed equation vs given equations
R-squared | 298.15K – 25C |  |  | 473.15K – 300C |  | 
Function | 2-parameter | Wagoner | 4-parameter | 2-parameter | Wagoner | 4-parameter
Average value | 0.838 | 0.955 | 0.993 | 0.674 | -2.49 | 1.0
R-square values > 0.98 | 82.35% | 49.41% | 91.76% | 0% | 0% | 100%

## Slide 36: Constitutive model – strain-rate dependent parameters calibration
Parameter calibration
Fix values for each parameter: Straight lines!!
=> Parameters evolving with strain
C1 | C2 | C3 | C4
-0.2019 | 1.2960 | 0.3338 | -0.0141
Average at 473.15K

## Slide 37: Constitutive model – strain-rate dependent parameters calibration
C1-C4 calibration
Low strain: Steep rise at small strain + gradual trends in the low-strain range
Intermediate strain: Microstructural transformation (elasticity to plasticity)
Large strain: Steady-state plastic deformation

## Slide 38: Constitutive model – strain-rate dependent parameters calibration
C1-C4 calibration
Chosen thresholds
Threshold1 = 0.002
Threshold2 = 0.04

## Slide 39: Constitutive model – strain-rate dependent parameters calibration
R-squared | 298.15K | 373.15K | 473.15K | 573.15K | 673.15K
C1 | 0.991 | 0.984 | 0.891 | 1.000 | 0.998
C2 | 0.994 | 0.992 | 0.963 | 0.993 | 0.859
C3 | 0.969 | 0.969 | 0.963 | 0.996 | 0.799
C4 | 0.998 | 0.996 | 1.000 | 0.994 | 0.995
Parameter calibration result – fixed thresholds
R-squared | 298.15K | 373.15K | 473.15K | 573.15K | 673.15K
C1 | 0.991 | 0.984 | 0.891 | 1.000 | 0.998
C2 | 0.994 | 0.992 | 0.963 | 0.993 | 0.859
C3 | 0.969 | 0.969 | 0.963 | 0.996 | 0.799
C4 | 0.998 | 0.996 | 1.000 | 0.994 | 0.995

## Slide 40: Constitutive model – strain-rate dependent parameters calibration
Stress validation result – fix thresholds
R-squared | 298.15K | 373.15K | 473.15K | 573.15K | 673.15K
R-squared values > 0.8 | 12.94% | 32.94% | 83.53% | 44.71% | 10.59%
Average R-squared | -21.72 | -527.39 | 0.82 | 0.56 | -179.96

## Slide 41: Constitutive model – strain-rate dependent parameters calibration
Limitation
Initial guess: Optimize initial guess by studying function shapes and behavior
C1-C4 function optimization: Focus on C3 and C4
Proposed function contains non-linear terms that are highly sensitive
Good R-squared only indicates how well the model fits the provided data but doesn’t ensure the parameters generalize well
Potential improvement
R-squared | 298.15K | 473.15K
C1 | 0.991 | 0.891
C2 | 0.994 | 0.963
C3 | 0.969 | 0.963
C4 | 0.998 | 1.000
Good prediction >< Bad validation?

## Slide 42: Back up C2 and C4 trend

## Slide 43: Machine Learning – coupled for temperature and strain-rate dependency
Develop Long Short-Term Memory (LSTM) model to predict stress-strain behavior using experimental data.
Conduct optimization and validation to ensure the model's accuracy and reliability.

## Slide 44: Challenges and Solutions
Challenges | Solutions
Dynamic range of data: Difficulty in capturing behavior over a wide range of strain, strain rates, and temperatures. | Employ logarithmic scaling and normalization techniques.
Computational cost: Training LSTMs with complex architectures can be computationally expensive. | Use CSC to accelerate training.
Hyperparameter tuning: Choosing the best combination of hyperparameters (e.g. number of neurons, etc.). | Automate tuning using grid search RandomizedSearchCV
Extrapolation issues: The model may struggle to predict stress-strain behavior outside the training data range. | Combine machine learning with physical models to improve generalization.
Interpretability: Understanding the LSTM's decision-making process can be challenging in physical applications. | Analyze feature importance to provide insights.

## Slide 45: Long Short-Term Memory (LSTM)
Model Architecture
Optimizer: Adam
Loss function: MSE
Activation: ReLU
Epochs: 50
Batch size: 32
*Visualize using NN-SVG Publication-ready NN-architecture schematics. NN-SVG is a tool for creating Neural Network (NN) architecture drawings parametrically rather than manually.
Flow Curves for training and testing set
Implement and training model
Training and testing results
Analysis the prediction of model
Hyperparameter tuning for LSTM model
Progress
Notes: Timesteps = 1

## Slide 46: Evaluation of Results
Training – 8 FCs Testing
Training set size (FC) | 8 | 12 | 15 | 16 | 17 | 18 | 19
R2 for testing set | 0.8686 |  |  |  |  |  | 
The model's performance is evaluated using Mean Squared Error (MSE) and R-squared (R²) metrics.

## Slide 47: Evaluation of Results
Training – 16 FCs Testing
Training set size (FC) | 8 | 12 | 15 | 16 | 17 | 18 | 19
R2 for testing set | 0.8686 | 0.9626 | 0.9754 | 0.9927 |  |  | 
The model's performance is evaluated using Mean Squared Error (MSE) and R-squared (R²) metrics.

## Slide 48: Evaluation of Results
Training – 19 FCs Testing
Training set size (FC) | 8 | 12 | 15 | 16 | 17 | 18 | 19
R2 for testing set | 0.8686 | 0.9626 | 0.9754 | 0.9927 | 0.9932 | 0.9954 | 0.9960
The model's performance is evaluated using Mean Squared Error (MSE) and R-squared (R²) metrics.

## Slide 49: Machine Learning – coupled for temperature and strain-rate dependency
The mechanical response of materials varies with temperature and strain rate due to thermal softening and dynamic strain aging (DSA) effects.
Machine learning or Long Short-Term Memory (LSTM) models are highly effective in accurately predicting the dynamic patterns of flow curves.
Flow curves behaviors under different temperature and strain rate conditions

## Slide 50: Validation
Validation for Machine Learning model
Generate data for 773.15K at StrRt0.0001 and RD
Run Abaqus simulation with generated data
Extract ODB file using Abaqus CAE, then compare with experimental data

## Slide 51: Validation
Validation for the Constitutive model
Method 1:
Run the model to yield data for material properties
Run Abaqus simulation with the material input

## Slide 52: Validation
Validation for Constitutive model
Method 2:
Make two separate VUMAT subroutine files: one with temperature function, one with strain-rate function
Include calibrated parameters in material properties input
Run Abaqus simulations with corresponding input and subroutine
enHill-VUMAT-TmpDpn.f
enHill-VUMAT-StrRtDpn.f
Material_TmpDpm.inp
Material_StrRtDpn.inp
CSC

## Slide 53: Comparison: Constitutive model vs LSTM model
 | Constitutive model | LSTM model
Accuracy (R-squared) | Temperature: 0.973 Strain rate: 0.82 | 0.996
Development effort | Temperature calibration: 1 developer, 2 assistants Strain-rate calibration: 1 developer, 2 assistants Many trials and errors with initial guess and function shape | 1 developer, 1 assistant Some trials and errors with choosing the right training/testing ratio
Development time | 8 weeks | 3 weeks
Usability | Physical meaning Easy and straight forward to use | No physical meaning Need some deployment
=> Machine learning (LSTM) model is more efficient given that the developer prior knowledge in ML. Not as much knowledge about MSE is needed.
=> Constitutive model is less efficient but it provides a mathematical model that is easy to interpret and understand.

## Slide 54: Summary
Literature Research
Material behavior and parameter identification.
Polynomial functions and fitting quality.
Flow Curve Fitting
Code development for flow curve and r-values
Preparation for temperature & strain rate calibration.
Temperature Dependent Model
Study existing thermal equations.
Proposed new thermal equations.
Optimized parameters, validated fitting model (R² = 0.972).
Constitutive model
Machine learning model
Strain Rate Dependent Mode
Study existing strain-rate equations.
Proposed new strain-rate equations.
Optimized parameters, validated fitting model (R² = 0.82).
Complete Model Validation
Subroutine files for temperature and strain rate dependence.
Couple Temperature and Strain Rate Dependency
Proposed LSTM model to predict stress-strain curves.
Validate the prediction with high accuracy (R² = 0.996).
Literature Research​
Material behavior under varying conditions​
ML/DL model

## Slide 55: Summary
Key results:
- Constitutive model:
+ Temperature calibration: R² = 0.973
+ Strain-rate calibration: R² = 0.82
Machine learning model:
+ Accuracy: 0.996